	                 Product
	장점/Remarks

	Star Tech UVA 4101:

Fast Track UV Cure Glass Adhesive
- A low viscosity acrylic adhesive formulated for fast cure on glass to glass bearing substrates even under low power UV lamp systems.  


	- This product can withstand over 30 dishwasher cycles and a –50 degree Celsius soak test with no detrimental effects. 

- This product can be used with automated or manual dispensing equipment.  

	Star Tech UVA 4102:

UV Cure Acrylate Adhesive for Lead Termination

- Ultraviolet curable compound that can be used in the adhesion of paper, PVC, styrene, acrylates, polycarbonates and rubber.
	- This product has a smooth, medium viscosity that keeps the compound from migrating during the application process. 



	Star Tech UVA 4103:

Medical Class VI Approved UV Cure Acrylic Adhesive

- Low viscosity acrylic adhesive that provides fast cure even when using a low power UV lamp system while providing minimal shrinkage.
	- This product demonstrates excellent adhesion to substrates such as PVC, steel, brass, aluminum, glass, tinned copper wire, epoxy and phenolic.  

- This product carries medical class VI approval.  

	Star Tech UNV UVA 4104:

Fast Tack UV Cure wire tack Compound

- Compound formulated for use on epoxy and phenolic PC boards, high-density paper, glass, plastic, and nylon surfaces.  
	- This product is designed to cure under low power UV lights in the user-friendly “A band” range.  

- This product has a viscosity of 10,000 cps with superior wetting ability on plastic, glass, or metal substrates.  


Star Technology is a formulator and compounder of a wide variety of reactive adhesives, coatings and encapsulation products. The chemistries of these products span the epoxy, urethane, acrylic and water base technologies.
	Star Tech UVA 4107:

Soft & Flexible Polymer for Adhesion and 

Potting:

- Compound made for use in the electronic

and mechanical assembly markets.  

- Typical applications include mechanical bumpers and shock absorbers, wire tack adhesives, potting or joining of delicate electronic components.  
	- This product cures rapidly under low powered UV lamps to yield a soft pliable rubber like elastomer with mechanical properties rivaling those of silicone elastomers. 

- This product adheres to substrates such as nylon, ABS, glass, polystyrene, steel, copper aluminum, etc.  



	Star Tech UVA 4109:

UV Cure Acrylic Doming Compound 

- Compound made for use in doming over decals, logos and standard decoupage applications.  
	- Can easily produce dome heads 0.03” to 0.06” above the substrate surface on most surfaces.  

- Cure can be achieved at rates of 50 linear ft. per minute.  

	Star Tech UVA 4110:

Fast Tack UV Cure Acrylic Adhesive
- Adhesive formulated for fast cure even under low power UV lamp systems while providing minimal shrinkage.  

- It is a thixotropic version of Star Tech UVA 4103.
	-This product demonstrates excellent adhesion to substrates such as ferrite, polycarbonate, styrene, acrylic, PVC, steel, brass, aluminum, glass, tinned copper wire, epoxy and phenolic.    

	Star Tech UVE 4050:

UV Cure Epoxy Resin

-Rigid and impact resistant, UV curable epoxy resin.  

- Holds a medium viscosity of 11,000 cps. 

- One of the hardest among Star Tech’s UV cure   epoxies with a shore hardness of 89D.
	- Possesses all the chemical resistance and tenacity of standard two part and heat cured epoxy compounds.  

- 100 percent solids product and contains no solvents or un-reactive diluents.  

- There is no problem with oxygen inhibition causing loss of cure or tackiness at the surface of the adhesive.

	Star Tech UVE 4052:

Thixotropic UV Cure Epoxy
-Thixotropic version of Star Tech’s UVE 4050 that allows the adhesive to adhere to a vertical surface with minimal sag.  


	-Contains no solvents or un-reactive diluents.  

-Product has been enhanced to improve adhesion to hard to stick to substrates such as glass, ceramic and silica containing substrates.  

	Star Tech UV4101:

Low Viscosity UV Cure Epoxy
-Formulated with a low viscosity, which will allow thorough wetting of any substrates.  
	-Formulated for greater impact resistance and flexibility than Star Tech’s UV 4050.  

-This product is ideal for intricate potting and encapsulation projects.  

	Star Tech UVE 4106:

UV Cure Epoxy Wire Tack Compound
-A high viscosity, medium thixotropy UV cure epoxy adhesive, similar to UVE 4101.  
	- Adhesion of this product to substrates such as tinned copper wire, epoxy, phenolic and polyamides are excellent.  

	Star Tech UVE 4107:

Soft & Flexible UV Cure Epoxy
- A UV cure epoxy adhesive and potting compound with a medium viscosity of 2000 cps.  

- It is the softest of the UV cure epoxy resin systems Start Tech currently have.  
	- Excellent for potting and delicate electrical components.  

- Adhesion to substrates such as tinned copper wire, epoxy, phenolic and polyamides are excellent.  

	Start tech VLE 4105:

Visible Light Cure Epoxy resin
- Low viscosity epoxy resin that can be cured with visible light.  

- Well suited for applications where UV light cured products are undesirable or impractical.  
	- Light in the 400-550 nm range will cure this product to a hard surface.  

- Moisture resistant and can withstand high heat applications.  

	Star Tech UVA 4000

UV/Room Temp. Epoxy for Encapsulation and Potting
- Designed for applications, which require a surface cure or skinning of the epoxy with UV light and then a later, room temperature curing of the deeper or shadowed resin.  
	- Applicable in potting, encapsulation and fast tack adhesive applications.  


