                                  SPECIFICATION

Coal grade  - D                    Indices                             Granular composition, mm

                                            2,8%                                                +50

                                            28,8%                                              25-50

                                            44,4%                                              13-25

                                            12,8%                                              1-13

                                            11,2%                                               0-1

Proximate analysis 

Total moisture                    11,0%

Ash on air dry basis            17,0%

Moisture in the analysis

sample (air dry basis)         3,5%

Total sulphur on air dry

basis                                   1,2%

Volatile matter on air

Dry basis                            37%

Gross calorific value

On air dry basis                 6200-7000 kcal/kg

Fixed carbon                      52,2%

Chlorine                             0,002%

Ultimate analysis of organic matter

Carbon                               77,8%

Hydrogen                           5,7%
Nitrogen                             2,1%

Oxygen                               12,8%

Chloride                             0,03%

Phosphorus                        0,005%

Fusibility of ash

Initial deformation temperature   1310C

Softening temperature                  1370C

Fluid temperature                         1390C

Chemical composition of ash

SiO2                                 67,1%

Al2O3                              19,2%

CaO                                  2,2%

Fe2O3                              2,5%

MgO                                1,6%

K2O                                 0,7%

Na2O                               0,01%

TiO2                                0,1%

MnO2                              0,01%

SO3                                 4,4%

P2O5                               0,2%

Hard grove grindability index               42

State Standarts Classification 25543     D,DB 0404601

Crucible swelling number                     1

Roga index                                            14

Plastometric indices                              X-46, Y-6
Gray-king coke type                               B
